## Slide 1: Phase Field Modeling of Thin Film Ferroelectrics

## Slide 2: Notation
Subscripted comma indicates differentiation with respect to coordinate axis
Repeated indices  Summation
Hats indicate Fourier space function

## Slide 3: Phase Field Model
Minimization of free energy
Energy Terms:
  Landau
  …

## Slide 4: Elastic Energy
Electrostriction + Elastic
Eigenstrain method
Physical interpretation = Eshelby Inclusions
  Stress free transformation generates an eigenstrain
  Allow relaxation of inclusion in stress free condition
  Squeeze the inclusion back into the bulk
  Squeezing necessitates creation of surface tractions
  Once the inclusion is put back in, surface tractions become body forces
  Cauchy equlibirum 
Homogenous and Hetereogenous strain
  Homogenous = macroscopic deformation
  We assume that in our simulation volume the heterogenous strain blah blah blah

## Slide 5: Eshelby Inclusions

## Slide 6
Matrix
Inclusion
1.
2.
3.
Inclusion undergoes stress free expansion with an associated strain of
4.
Application of surface traction , where , to restore the inclusion back to its original shape. The elastic strain generated by the surface traction is .
5.
Insert the inclusion back into the matrix. The surface tractions are removed by defining a body force that acts on the surface of the inclusion. A displacement field and strain are generated in response to this body force. By defining , mechanical equilibrium can be solved.
Remove inclusion from the matrix
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
No elastic strains exist in the material
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Total Stress and Strain
Elastic Stress and Strain
Matrix | Inclusion
Matrix | Inclusion

## Slide 7
Matrix
Inclusion
1.
2.
3.
4.
5.
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Matrix | Inclusion
Elastic Stress and Strain
Matrix | Inclusion
Matrix | Inclusion

## Slide 9: Macroscopic Thin Film Boundary Conditions

## Slide 10: Relaxation of Heterogenous Strain
Solve for ,
Calculate
Plug back into LGD functional

## Slide 11: Thin Film Boundary Conditions for Heterogenous Strain
  Periodic in x1 and x2
    Strain at substrate is zero
    Stress free surface
Solve by breaking up into two parts
  Homogenous solution, RHS = 0
  Particular solution, RHS = eigenstrain
  Adapt the total solution (homogenous + particular) to fit the BC via coefficients

## Slide 13: Particular Solution
Easily done in Fourier space
Use Green’s elastic tensor
Fourier Transform ()
  Green’s elastic tensor
  Position dependent tensor in Fourier space

## Slide 14: Verification of Particular Solution
Expand the RHS and LHS terms… see if they equal…

## Slide 15: Homogenous Solution
2D Fourier transform
Math simplifications…
We get 1D ODEs in terms of x3 for each point
Use matrix methods to solve the 1D ODE
Collect the solutions and 2D IFFT along each x3 slice to get the full solution

## Slide 16: MATH… Want to solve that messy equation, guess an exponential… and we get simplifications and an eigenvalue equation…

## Slide 17: The General Solution to the Homogenous Problem
2D Fourier Transform
Vector: 3 components to the displacement vector
General Solution
Fit coefficients to boundary conditions
Dependent on and unique to k space vector

## Slide 18: Verification
Expand the LHS term, i = 1, 2, 3
  3 Equations
i = 1 Equation:

## Slide 19: Checking…
C11 = 27.50 * 1e10
C12 = 17.90 * 1e10
C44 = 5.43 * 1e10
64 * 64 * 64 Grid
  Total length of 1 nm in x, y, and z directions
General solution, set all coefficients to zero except a few

## Slide 20
x3 = 0
x3 = 0
What we are plotting: 2D k-space in plane, constant x3 cross section, z axis = magnitude of the function value at that specific point

## Slide 21: The Total…
Not exactly zero
But considering our initial inputs (~1e16), dramatic reduction in magnitude  Essentially zero

## Slide 22: K Space Origin
Eigenvalue solution doesn’t work
1D Exponential not a solution!!
Remember 2D Fourier Space

## Slide 24: Verifying Stress Free Surface

## Slide 26: Semi-Implicit Fourier Spectral Method
Fourier Transform
  Transforms your signal periodically
  FFT  discrete, numerical implementation
  Derivatives become multiplication  Numerically more stable
Semi-implicit Fourier Spectral Method
  Treat the gradient terms implicitly  More stable [LQ Chen]
  Can expand the time dependence to get greater time accuracy but at the cost of computational speed
    https://en.wikipedia.org/wiki/Linear_multistep_method

## Slide 28: For a Real Case u ~ 0 at substrate

## Slide 29: Stress free surface verification

## Slide 31
x3 = 0
x3 = 0
What we are plotting: 2D k-space in plane, constant x3 cross section, z axis = magnitude of the function value at that specific point